FORMSHIELD PURE

Low VOC, Oil Based Form Release Agent

{Note to Specifier: The paragraphs below are meant to be incorporated into Part 2 of a standard CSI 3 Part Format specification, the General Structural Notes, or directly onto the plans. They must be carefully reviewed and edited by a qualified design professional to meet the requirements of the project and governing building codes. Coordinate with other specification sections and drawings.}

PART 2:	PRODUCTS

2.__	PRODUCTS

A.	Low VOC, Oil Based Form Release Agent:  Maximum VOC content 90 g/L. Compliant with Federal, OTC, California, and Maricopa County regulations.

1.	Product:

a)	Euclid Chemical Company (The); Formshield Pure, www.euclidchemical.com

2.__	MANUFACTURER

A.	Manufacturer shall have ISO 9001 Quality Certification. To ensure compatibility all products shall be from the same manufacturer.