EUCON VANDEX AM-10

Integral Crystalline Waterproofing Admixture

{Note to Specifier: The paragraphs below are meant to be incorporated into Part 2 of a standard CSI 3 Part Format specification (normally 03 30 00), the General Structural Notes, or directly onto the plans. They must be carefully reviewed and edited by a qualified design professional to meet the requirements of the project and governing building codes. Coordinate with other specification sections and drawings. In no case shall these Guide Specifications be considered to be Contract Documents or serve as installation instructions for the product being discussed. In any cases of discrepancy the manufacturer's most recently published data sheet shall take precedent.}

PART 2:	PRODUCTS

2.__	ADMIXTURES

A.	Crystalline Waterproofing Admixture: Integral crystalline admixture specifically formulated to interact with capillary pore structures to provide a waterproofing system that is a permanent part of the concrete matrix. Admixture shall provide the following properties:

Water Penetration per DIN 1048				40% Reduction at 72 psi.

Water Permeability per CRD C48-92			>70% Reduction at 200 psi

Capillary Absorption per ASTM C-1585			>40% Reduction

Compressive Strength per ASTM C-39			Equal to and up to 8% increase

Resistance to Chloride Penetration per ASTM C-1202	10% improvement

Length Change per ASTM C-157			Up to 20% Reduction

1.	Basis of Design Product:

a)	Euclid Chemical Company (The); Vandex AM-10 or Vandex AM10L, www.euclidchemical.com

2.__	MANUFACTURER

A.	Manufacturer shall have ISO 9001 Quality Certification. To ensure compatibility all admixtures shall be from the same manufacturer.