LEVEL MAGIC LIGHT WEIGHT

Cement based, self leveling, high strength underlayment designed for leveling floors from feather edge to 1” deep without the adding the weight of traditional underlayments.

{Note to Specifier: The paragraphs below are meant to be incorporated into Parts 2 and 3 of a standard CSI 3 Part Format specification, project’s General Structural Notes or directly onto the plans. They must be carefully reviewed by a qualified design professional and edited to meet the particular requirements of the project at hand, assure compliance with any governing building codes, and coordinate with other specification sections and drawings.}

PART 2.0:	PRODUCT

2.__	BONDING AGENT/PRIMER

{REPAIR NOTE: Required Bonding Agents}

{Note to Specifier: Certain bonding agents, adhesives and/or primers are recommended with this product. Choose a recommended bonding agent/primer from the data sheet and insert here.

{PRODUCT}

2.__	CEMENTITIOUS REPAIR MORTAR

A.	Single component, self leveling light weight underlayment suitable for applications from featheredge to 1” in depth and requiring only the addition of water. Material shall have the following properties:

1.	Compressive Strength per ASTM C 109

Age			Strength

7 days		3,000 psi

28 days		4,000 psi

2.	Flammability ASTM E 84

Flame Spread		0

Flame Contribution	0

Smoke Development	0

3. 	Unit weight:	80 lbs. per cu. ft.

4.	Product:

a)	Euclid Chemical Company (The); Level Magic Light Weight www.euclidchemical.com

B.	Manufacturer shall have ISO 9001 Quality Certification. To ensure compatibility all admixtures shall be from the same manufacturer.

C.	To ensure compatibility bonding agent and curing compound if used shall be from same manufacturer as repair mortar.

PART 3.0:	EXECUTION

3.___	SURFACE PREPARATION

{CONCRETE PREP AND CLEANING NOTE}

A.     Concrete Preparation and Cleaning: Areas to receive concrete repair shall be structurally sound and free from deteriorated concrete, dust, dirt, debris, loosened concrete, paint, oil, efflorescence, laitance, and other contaminants, and shall have a minimum Concrete Surface Profile CSP equal to that recommended by the repair mortar manufacturer per ICRI Guideline 310.2.

3.___	REPAIR MORTAR APPLICATION:

{SELF LEVELING UNDERLAYMENT APPLICATION NOTE}

A.	Self Leveling Cementitious Material Application: Mix and apply material in continuous manner per manufacturer’s published recommendations so as to provide smooth uniform surface.