EUCOREPAIR SMOOTH

Polymer Modified, Cementitious Finishing Material

EUCOREPAIR SMOOTH is a single-component, polymer-modified, cement based

material used for achieving a smooth finish on precast, cast-in-place, tilt-up or

other unfinished concrete surfaces with imperfections.

{Note to Specifier: The paragraphs below are meant to be incorporated into Parts 2 and 3 of a standard CSI 3 Part Format specification, project’s General Structural Notes or directly onto the plans. They must be carefully reviewed by a qualified design professional and edited to meet the particular requirements of the project at hand, assure compliance with any governing building codes, and coordinate with other specification sections and drawings. In no case shall these Guide Specifications be considered to be Contract Documents or serve as installation instructions for the product being discussed. In any cases of discrepancy the manufacturer's most recently published data sheet shall take precedent.}

PART 2.0	PRODUCTS

2.__	CEMENTITIOUS REPAIR MORTAR

A.	Trowelable Vertical and Overhead Cementitious Skim Coat from featheredge to 3/8” (9 mm): Cement-based, one component, polymer modified, trowelable finish coat for concrete surfaces and suitable for interior or exterior use. Minimum 4,000 psi (28 MPa) Compressive strength at 28 days when measured in accordance with ASTM C109/109M.

1.	Basis of Design Product:

- Euclid Chemical Company (The); EUCOREPAIR SMOOTH

B.	Manufacturer shall have ISO 9001 Quality Certification.

C.	To ensure compatibility bonding agent and curing compound where used shall be from same manufacturer as repair mortar.

PART 3.0	EXECUTION

3.___	SURFACE PREPARATION

A.	Concrete Preparation and Cleaning: Areas to receive concrete repair shall be structurally sound and free from deteriorated concrete, dust, dirt, debris, loosened concrete and aggregates, bruised concrete substrate weakened by microcracking, paint, oil, efflorescence, laitance, and other contaminants, and shall have a minimum Concrete Surface Profile CSP equal to that recommended by the repair mortar manufacturer per ICRI Guideline 310.2.

3.___	REPAIR MORTAR APPLICATION:

A.	At areas where a bonding agent has not been specified, the saturated-surface dry (SSD) concrete shall be primed with a scrub coat of the specified repair mortar.

1.	Soak the repair area with potable water to achieve a saturated-surface dry (SSD) condition.

2.	The repair mortar must be placed before the scrub coat dries out.

B.	Cementitious Skim Coat Application: Mix and apply cementitious skim coat per manufacturer’s recommendations within the open time of the product scrub coat or any bonding agents.

3.___	CURING

- Cure in accordance with manufacturer’s instructions on literature.

END GUIDE SPEC