VANDEX CONSTRUCTION JOINT TAPE

Waterproofing strip for static joints and cracks

{Note to Specifier: The paragraphs below are meant to be incorporated into Parts 2 and 3 of a standard CSI 3 Part Format specification, project’s General Structural Notes or directly onto the plans. They must be carefully reviewed by a qualified design professional and edited to meet the particular requirements of the project at hand, assure compliance with any governing building codes, and coordinate with other specification sections and drawings.}

PART 2.0:	PRODUCT

1.__	Synthetic rubber “tape” used to provide a permanent waterproof seal over static joints and cracks.

{Note to Specifier: All of the material properties shown in the sub paragraphs below are not typically applicable on every project. They are listed here in order to allow the design professional to review and edit the information according to the particular project parameters for which the product will be used.}

A.	VANDEX CONSTRUCTION JOINT TAPE is used in conjunction with VANDEX BB 75 or VANDEX CEMELAST to provide a permanent waterproof seal over static joints and cracks on either the positive or negative side of a substrate.

1.	Construction Joint Tape shall be alkali resistant

2.	Construction Joint Tape shall be reinforced with a flexible polyester fabric

3.	Product:

a)	Euclid Chemical Company (The), VANDEX CONSTRUCTION JOINT TAPE.

www.euclidchemical.com

B.	Manufacturer shall have ISO 9001 Quality Certification. To ensure compatibility all associated products shall be from the same manufacturer.

C.	To ensure compatibility, all materials used shall be from same manufacturer.

2.___	CURING

{Euclid Chemical recommends the following for maximum effectiveness}

- When using VANDEX BB 75 Mortar to adhere Vandex Construction Joint Tape, it is essential that the material be wet cured for a minimum of 5 days.  Once VANDEX BB 75 has hardened sufficiently, standard wet curing processes may be utilized. Wet or fog spray, or cover with polyethylene sheeting, wet burlap or burlene if a subsequent topical treatment is to be applied.  The mortar must be protected from rain during the first 24 hours and be protected from frost for at least 5 days.  Use insulation blankets if necessary.  Backfilling can occur 3 days after placement.

- When using VANDEX CEMELAST Elasticized Waterproof Coating to adhere Vandex Construction Tape, VANDEX CEMELAST requires no curing procedures due to the enhancement from the VANDEX CEMELAST LIQUID. VANDEX CEMELAST must be protected from rain during the first 24 hours and be protected from frost for at least 5 days. Use insulation blankets if necessary. Backfilling can occur 3 days after placement.

PART 3.0:	EXECUTION

3.___	SURFACE PREPARATION

A.	The surface should be structurally sound, clean and free of dirt, oil and other contaminants including curing compounds, form release agents, old coatings, paint and efflorescence.  New concrete and masonry must be cured a minimum of 7 days.  All concrete laitance must be removed.  Mechanically prepare the concrete to a CSP 3-5 in accordance with ICRI Guideline 310.2.  Concrete honeycombs, cavities, joints, cracks, voids, tie holes and other defects must be opened and routed to a ¾”depth or to sound material.  No active water leaks should be present at the time of the application of VANDEX CONSTRUCTION TAPE.  Use SPEED PLUG, VANDEX PLUG, or VANDEX SUPER mixed with VANDEX QUICKBINDER to stop all active leaks.  Any surface defects need to be addressed with the application of VANDEX UNI MORTAR 1 ZSR. If the VANDEX CONSTRUCTION JOINT TAPE is going to be used to treat cracks and joints on the negative side, rout out the cracks and joints to 3/4” in depth and fill with VANDEX UNI MORTAR 1 ZSR. Once prepared, the substrate needs to be soaked with water to a saturated, surface dry (SSD) condition just prior to the application of the material.

4.___	CONSTRUCTION JOINT TAPE APPLICATION:

A.	VANDEX CONSTRUCTION JOINT TAPE requires no mixing or preparation; however the VANDEX slurry materials used to adhere the tape to the substrate require mixing. Please refer to the technical data sheets of either VANDEX BB 75 or VANDEX CEMELAST for proper mixing and application instructions.

B.	After preparing the joint or crack as described above, follow the directions on the VANDEX slurry material technical data sheet for mixing and placement. Apply the first coat of slurry material and be sure to extend the application of the VANDEX slurry material at least 3/8” beyond the width of the tape in each direction. Position the tape over the applied coating and embed properly, making sure the fabric webbing on the edges gets fully embedded. Overcoat the tape with a second lift of VANDEX slurry mortar and smooth with a trowel or damp brush. In the event the VANDEX CONSTRUCTION JOINT TAPE and slurry are applied for negative side protection, mechanical bracing will be required if hydrostatic pressure is present through the crack or joint in the substrate.